Thermodynamic measurements of lithiation in graphite
-galvanostatic, GITT, entropy, enthalpy

---
Motivation
- Need good quality data for model validation: several gaps in the literature:
  - Half cell Li/graphite (OCV) measurements at variable T, conducted at sufficiently slow C-rate to extract meaningful thermodynamic parameters. Last systematic variable T experiments done by Aurbach circa 2000:
    - Slow rate CV and PITT (3 electrode cell): but no data below 25 degrees C.
    - Data from Argentina group: all done at room T.
  - Apparent hysteresis between charge and discharge profiles – why?
  - Role of surface versus bulk in low SOC features, and effect of T – more data needed to validate hypotheses.
  - Entropy information:
    - Existing data from Yazami – missing data at high SOC, experiments conducted with only one central temperature. Possible issues with experimental protocols.
    - Very little analysis done to interpret the profiles – no modelling.
    - Enthalpy profiles (from same experiments): could shed insight into the nature of the transitions between different stages (two phase versus solid solution) and low SOC transitions.
    - Parameters from inelastic neutron scattering experiments (Debye temperatures) exist already: possibility to get quantitative information on vibrational as well as configurational entropy and their T dependence.
Controlled temperature Li/graphite coin cell experiments, in combination with atomistic-based models, have the potential to address all or most of the above!

---
Experimental plan
- We have a starting sample with a mean CHECK 20 micron particle size (from Sigma-Aldrich).
  - Conveniently, same graphite used by Manuel Otero in Cordoba.
  - Synthetic graphite sample – and readily available!
- Richard Fields (Manchester) has agreed to perform molecular sieving to control the particle size distribution (more small particles) and to perform BET analysis on these distributions:
  - Change the mean surface/area to volume ratio.
  - Experiments in Cordoba showed ball milling introduces extra oxygenated defects in between graphene planes.
- Meanwhile, Miriam and Cindy made coins cells here with the raw 20 micron sample, with intentionally low mass loading.
- So far experiments have been conducted at 25 degrees, or a central T = 25 degrees, but evental aim is to examine high and low T to provide maximum data to validate the models.

---
Structure (20 microns, 25 degree central T)
- Part 1: preformation cycles (C/10).
- Part 2: slower (C/50) galvanostatic profiles.
- Part 3: dQ/dV and dV/dQ from C/50.
- Part 4: high resolution GITT (charge and discharge)
- Part 5: IN PROGRESS high resolution entropy profiling (charge and discharge)
- (Note all C rates are based on the theoretical capacity of 372 mAh/g)

---
Part 1: preformation cycles
- These are standard protocols that we adopted after consulting with Manuel Otero (Cordoba) and Konstantinos Antonopoulos (TUM).
- Was done as first thing on each cell:
  - to ensure stable SEI formation
  - To check the general electrochemistry and feaures of graphite before moving on to the much slower measurements.
  - All preformation done at 25 degrees C.
  - A 20 min rest period was performed between each charge and discharge.

---
Results: preformation (C/10)
T = 25 degrees

---
Capacity 1st and 2nd cycles (C/10)
Discharge
Charge
Cell 5
T = 25 degrees
All cells showed an irreversible loss of capacity after first discharge: SEI formation

---
Part 2: C/50 (after preformation cycles)
T = 25 degrees, all performed after constant voltage step at 1.5 V
for at least 30 minutes

---
Capacity (C/50)
Second cycle
First cycle
T = 25 degrees
Cell 1

---
Determination of max and min state of charge (SOC)
- Tricky:
  - High SOC limit: < 0 V Li. Therefore impossible to achieve theoretical 372 mAh/g based on perfect LiC6 structure.
  - Low SOC limit – possible overlap with interfacial processes (SEI formation may not be completely irreversible as commonly assumed).
  - Assume the theoretical capacity as the maximum, to enable a comparison with models.
  - For now, assumed the cutoff at 1.5 V corresponds to the min SOC. This may result in some small error, reflected in the position of the Stage I – Stage II plateau (theoretcially at 50% SOC).

---
Voltage versus SOC (C/50)
Cell 3
Cell 8

---
Part 3: galvanostatic intermittant titration technique (GITT)
One set of experiments with C/10 (12 minutes, 50 steps each charge and discharge) followed by variable relaxation time (20 mins, 40 mins, 60 mins)
20 mins relaxation
40 mins relaxation
60 mins relaxation

---
Effect of relaxation time
c.f. galvanostatic results at C/50
Note these cells were done with high resolution!

---
Part 3: dQ/dV and dV/dQ
- These were just done on the second discharge and charge cycles at C/50.
- Smoothing was applied with the following parameters: ADD LATER

---
Part 4: GITT
- Following the procedure adopted in this paper: discharge for 12 minutes, followed by open circuit relaxation at variable times: 20 minutes, 40 minutes, 60 minutes.
- The high resolution data were conducted with relaxation time = 20 minutes, and discharge steps 12 minutes at C/50 (a total of nearly 250 points each for charge and discharge).
- So far conducted at T = 25 degrees, but will be repeated at other temperatures.

---
Effect of relaxation time